| Plastic | Examples | Good | Bad |
| --- | --- | --- | --- |
| PE (Polyethylene) Crystalline | -RLDPE-radically low density polyethylene -VLPE – Field Covers -LLDPE-(linear low) Plastic Bags -LDPE-Food Container Lids -HDPE-Recycle Box -UHMW-UHDPE high wear apps -cosmetics | -Low cost -Lightweight -Medium Gloss -Impact Resistance -Chemical Resist -Environmental Stress Cracking (ESC) Resist -Food Safe | -Low UV resist ( inhibitor and colour variations) -low E Modulus (not stiff) -Expands in high temp -high permeability to gas/solvents -difficult to bond with glue |
| PS (Polystyrene) Amorphous | CD Case Plastic Utensils Styrofoam | -low cost -High Gloss -hard and stiff - easy to process -clear grade -good colourability -somewhat food safe (cold food) | -poor weather ability -brittle, low impact strength (especially homopolymer) -poor thermal stability -flammable -ESC with fats/oils -notch sensitive |
| SAN (Styrene Acrylontrile) Amorphous | Packaging Household (vacuum) Car break light Measuring cup | -Low cost -slightly yellow(acrylonitrile) -high gloss -wide range of opaque, transparent and smoky colours -highest E modulus (stiff) of styrenes -Food safe -chem resist | -poor weather -low UV resist -ESC -Brittle (tougher than PS, weaker than HIPS and ABS) |
| PMMA (Polymethyl Methacrylate) Amorphous | Drafting tools Display cases Soap dishes | -medium cost -very clear -scratch resist(coating of polysilicate) -High E modulus (stiff) -good ESC and UV resist | -notch sensitive -low impact strength |
| PC (Polycarbonate) Amorphous Thermoplastic | Car headlight Gardening tools | -good colourability -tough, strong, and stiff -impact resist -temp resist (keeps ^ at a wide range of temps) -scratch resist with gloss -creep resist -Engineering Thermoplastic -clear grade | -high cost -ESC with oils, grease, and chemicals -so stiff it cracks wih insert and self-tapping fasteners -BPA=not food safe (bad for hot food, cold food = questionable) |
| PSO (Polysulfone) Amorphous | Astronaut Helmet Microwave dish Milking Equipment (cow) | -durable in demanding performances -glossy -transparent and opaque grades -very high stable temperature control over range of temps -chemical resist -very food safe | -very high cost -difficult to colour -stress cracking with inserts -ESC |
| CA (Cellulose Acetate) Amorphous | CA-Screwdriver handle CAB-skylight CAP-toothbrush, steering wheel | -tactile quality -high gloss -good colourability -very clear grades -tough -mechanical strength, metal embedment | -high scratch resist -low creep resistance -low dimensional stability -water absorption (especially CA) -CAB-more weather able |
| TPE (Thermoplastic Elastomers) | ETE-shoes TPO-flippers Styrenic Types-razor, bike handle TPV-window wiper TPUS-Raincoat | -low to medium cost -properties of thermoset rubbers, with processing capabilities of thermoplastic polymers -Molded on delicate inserts -tough and wear (TPUs) -can be co-extruded or co-molded to combine hard and soft elastomers |  |
| PA (polyamide) (Nylon) Crystalline | Ski boots Clips Fishing line Wire twist ties | -moderate cost -surface similar to PE -milky white/opaque virgin colour (amorphous clear version) -high resist to oil and grease -high fatigue and creep resist -Stiff and tough -impact resist -low friction coefficient | -permeable to moisture, leads to dimensional instability -UV sensitive |
| EVA | Crocs Soccer balls Glue sticks Plastic wrap Puzzle mats | -low cost -flexible and tough -surface tactile/sticky -translucency changes with vinyl-acetate -good UV resist -impact strength -flexible when cold - | -more permeable than PE to gasses and water -Not food safe - |
| PUR thermoset | Clack trolley wheels Cable jackets Foam bed mat Shoe soles | -price depends on moderate to high thermoset -only dark colours -higher E modulus than rubber -high form stability, flexibility, and abrasion resist -good weather/chem resist -elastic at low temp | -UV cases it to yellow -not resistant to hot water/vapour |
| PF thermoset | Pot handle Knobs House foam insulation Power plugs | -high performance engineering or general purpose -Glossy and scratch resist -good stiffness -high temp resist -good chem resist -impact strength and mechanical properties | -virgin colour is brown -discolours in UV -not food safe -brittle if not mixed with fibers - |
| PVC Amorphous | Water pipes Key chains Window frames Fake leather (soft grade with plasticizers) | -low to medium cost -surface gloss and colourability -transparent grade -weather and UV resist -low permeability for gas, solvents and smells | -chlorine=not environmental -melts above 60 C |
| Polyester Thermoset | Clothing Ski poles/skis Tent pols | -low cost -made with resin and catalyst (2 part), generally mixed with fiber and fillers -good temp and weathering ability -chem and flame resist - | -brittle without fiberglass - |
| Fiberglass |  | -low cost -stiff -combines resin, or the matrix, with glass fibers |  |

V is also PVC****