Chapter 3: The Structure of Crystalline Solids

Fundamental Concepts

Crystalline: Repeating/periodic array of atoms; each atom bonds to nearest neighbor atoms.

Crystalline structure: Results in a lattice or three-dimensional arrangement of atoms

Unit cells

- Smallest repeat unit/entity of a lattice.

- Represents symmetry of the crystal structure.

- Basic structure unit/building block of crystal structure

- Defines the crystal structure by its geometry and atom positions

Co-ordination number

For each atom, it is the number of nearest-neighbors or touching atoms

Example: FCC:12, HCP:12, BCC:8

Atomic packing factor (APF):

APF=Volume of atoms in a unit cellTotal unit cell volume=VsVc

=0.74 for FCC or HCP

=0.68 (for BCC)

Atoms per unit cell

FCC     Face atoms= 6 x ½ =3           	4

Corners atoms = 8 x 1/8 =1

Examples:  Al, Ni, Cu, Au, Ag, Pb, Gamma (γ)-Iron

BCC     Body atom=1                         	2

Corners atoms = 8 x 1/8 =1

Examples: Cr, W, Alpha (α)-Iron, Delta (δ)- Iron, Mo, V, Na

SC       Corners atoms = 8 x 1/8 =1 	1

Metallic crystal structure

SC (Simple Cubic)

BCC

(Body-Centered Cubic)

FCC

(Face-Centered Cubic)

Where:

R = Radius of the atom

a = cube edge

a2 + a2 = (4R)2

2a2 = (4R)2 = 16R2

a = 2R √2

APF=Volume of atoms in a unit cellTotal unit cell volume=VsVc

Unit cell volume (Vc)=a3

=2R23

=16 2 R3

Vs=43π R3*4          4 atoms per unit cell

=163π R3

Total cell voleume Vc=16 2 R3

APF=VsVc=163πR3162 R3=0.74

a√3

a√2

Body Centered Cubic

All sides are equal to dimension “a”

a2 + a2 = 2a2

(a√2)2 + a2 = 3a2 = (4R)2

a√3= 4R

The Hexagonal Close-Packed

6 Atoms at top         		  12

6 Atoms at bottom

2 Centre face atoms

3 Midplane atoms

12 x 1/6 = 2

2 x 1/2  =  1     			  6 atoms/unit cell

Midplane  3

Co-ordinate number: 12 (HCP or FCC)

Atomic packaging factor (APF): 0.74

Examples: Cd, Zn, Mg, Ti

Density Computations

Density, 	ρ=nAVcNA

Where,

N   =  No. of atoms/unit cell

A   =  Atomic weight

Vc  =  Volume of unit cell

NA =  Avogadro’s number (6.023 x 1023/mole)

Example:

Copper has an atomic radius of 0.128 nm, an FCC crystal structure, and an atomic weight of 63.5 g/mol. Compute its theoretical density and compare the answer with its measured density.

Given:

Atomic radius = 0.128 nm (1.28 Ǻ)

Atomic weight = 63.5 g/mole

n = 4

ACU = 63.5 g/mol

Solution:

Unit cell volume = 16 R3√2

R = Atomic Radius

= 8.89 g/cm3

Close to 8.94 g/cm3 in the literature

Crystal system

x, y, z : Coordinate systems

a, b, c : Edge lengths

α, β, γ : Inter axial angles

Cubic system: a=b=c    α=β=γ=90°

Lattice parameter (e.g., a,b,c, α, β, γ)

determine the crystal system. There are seven

crystal systems which are Cubic, Tetragonal, Hexagonal, Rhombohedral (Trigonal), Monoclinic, Triclinic.

Crystallographic Direction

Steps:

- Choose a vector of convenient length

- Obtain vector projection on each of three axes (for the direction to be drawn, if necessary)

- Divide the three numbers by a common factor (if the indices are to be assigned) to reduce to the smallest integer values

- Use square brackets [  ]

Crystallographic Planes

Miller Indices (hkl)

Steps:

- Obtain lengths of planar intercepts for each axis.

- Take reciprocals

- Change the three numbers into a set of smallest integers (use a common factor )

- Enclose within parenthesis e.g., (012)

Tips:

1. Parallel planes have the same indices

2. An index 0(zero) implies the plane is parallel to that axis.

Cubic Crystal system

(   ) 	Plane

{   } 	Family of planes

[  ] 	Direction

<  > 	Family of directions

Example:

{111}:

Hexagonal Crystal system

[u’v’w’] ------->  [u v t w]

[0 1 0] ------->

u = n/3 (2u’ – v’)

e.g.,  u = n/3 (2 x0 – 1)

Where,  n=factor to convert into indices = 3

u= 			           = n/3 (0 -1)

v = n/3 (2v’ – u’)

Example: v = n/3 (2 x 1 -0)

= n/3 (2)

Where:

n = factor to convert into indices = 3

v = 2

t = - (u’ + v’)			u v t w =

Example:  t = -(0 + 1)

= -1 =

w = w’

c

a1, a2, a3  axes: 	all in basal plane (at 120° to each other)

Z-axis: 			Perpendicular to basal plane

[u’v’w’] ------->  [u v t w]

a b c                  a b z c

Miller -------> Miller-Bravais

u = n/3 (2u’ – v’)  	[0 1 0] ------->

v = n/3 (2v’ – u’)	 	u’v’w’  ---->     u v t w

t = - (u’ + v’)			u = (0 -1),  t = -(1),  v = 2,  w = 0

w = nw’

n=factor to convert into indices

Linear and Planar Atomic Densities

Linear density 		4R = a√3

BCC			a = 4R/√3

a√3

a√2

a

N

M

BCC LD 100=Distance occupieddistance available

=2Ra

=2R4R2

=0.866

X- Ray Diffraction

Interplanar

spacing

nλ=

Where,

n = an integer, order of reflection

= 1 (unless stated otherwise)

Bragg’s law of diffraction

nλ  = dhkl sinθ + dhklsinθ

= 2dhkl sinθ

For cubic system,		a2/d2 = h2 + k2 + l2

X-Ray Diffraction

nλ =

= path difference         		where n = integer = 1

= dhkl sinθ + dhklsinθ

= 2dhkl sinθ

a2/d2 = h2 + k2 + l2

(h + k + l) must be even: BCC    2, 4, 6, 8, 10, 12……

h k l: all odd or all even FCC 3, 4, 8, 11, 12, 16……..

If the ratio of the sin2θ values of the first two diffracting planes is 0.75, it is FCC structure. If it is 0.5, it is BCC structure.

λ=2d sinθ

=2a sinθh2+k2+l2

sin2θ= (λ2 (h2+k2+l2))/(4a2)

(sin2θ1)/(sin2θ2)=h12+k12+l12h22+k22+l22                 λ and a are constants

Example

Givens:

{211} Planes

aFe = 	0.2866 nm (2.866Å)

λ = 	0.1542 nm (1.542Å)

n = 1

Determine dhkl, 2θ (diffraction angle)

  - dhkl = a/ √ (h2 + k2 + l2)

= 0.2866 nm /√ (22 + 12 + 12)

= 0.1170 nm (1.170Å)

- sinθ=nλ2dhkl=1*0.15422*0.1170

θ=sin-10.659=41.22°

2θ=82.44°

Crystalline and Non-crystalline materials

Single crystal:		 No grain boundary

Polycrystalline: 	Several crystals

Anisotropy: 		Directionality in properties

Isotropy: 		No directionality

Modulus of elasticity (E), psi x 106 (MPa x 103)

|  |  | [100] | [110] | [111] |
| --- | --- | --- | --- | --- |
| FCC | Al | 9.2 | 10.5 | 11.0 |
|  |  | (63.7) | (72.6) | (76.1) |
| FCC | Cu | 9.7 | 18.9 | 27.7 |
|  |  | (66.7) | (130.3) | (191.1) |
| BCC | Fe | 18.1 | 30.5 | 39.6 |
|  |  | (125) | (210.5) | (272.7) |
| BCC | W | 55.8 | 55.8 | 55.8 |
|  |  | (384.6) | (384.6) | (384.6) |

Non-Crystalline

- Amorphous

- No systematic arrangement (regular) of atoms

Summary

- Crystalline –lattice

- Crystal system: BCC, FCC, HCP

- Planes, directions, packing

- X-Ray diffraction