Chapter 4: Imperfections in Solids

Introduction

- Metals

- Alloys

- Solid solutions

- New/second phase

- Solute (the guest)

- Solvent (the host)

Solid solutions

Substitutional solid solutions

Interstitial solid solutions

| Cu | Ni | Substitutional |
| --- | --- | --- |
| Dia: 1.28Å | Dia: 1.25 Å | Atomic size factor (difference in atomic radii: ±15%) |
|  |  | Electrochemical factor (must be close in periodic table otherwise intermetallic compound) |
| +1 | +2 | Relative valencies factor (higher valence metal dissolves in lower valence metal) |
| FCC | FCC | Same crystal structure, solid solution |

Defect: Irregularity

Point defects:

- Vacant lattice site: vacancy

- Addition atom crowding

- into an interstitial site

- Self-interstitial: same type of atom

No. of vacancies, 		Nv=Nexp (-QvkT)

Where:

N 	= no. of atomic sites

QV 	= Activation energy to form vacancy

T 	= Absolute temperature, K

k 	= Boltzmann constant

= 1.38 x 10-23 J/atom-K

= 8.62 x 10-5 ev/atom-K

R	= 8.31 J/mol-K 		(gas constant)

= 1.987 calories/mol-K

Example:

Calculate the number of vacancies per cubic meter of copper at 1000°C. The activation energy for vacancy formation is 0.9 ev/atom; the atomic weight and density (at 1000°C), for copper are 63.5 gm/mol and 8.4 gm/cm3 respectively.

Solution

N 	= No. of atomic sites/ cubic meter of copper

ACu 	= Atomic weight of copper

= 63.5 gm/mol

ρCu 	= Density of copper

= 8.4 gm/cm3

NA 	= Avogadro’s no.

= 6.023 x 1023 atoms/mol

N 	= NA ρCu/ACu

= 8.0 x 1028 atoms/m3

No. of vacancies at 1000 °C (1273 K)

Nv=Nexp (-QvkT)

QV 	= 0.9 ev/atom

N 	= 8.0 x 1028 atom/m3

k 	= 8.62 x 10-5 ev/K

T 	= 1273 K

Therefore,

NV 	= 2.2 x 1025 vacancies/m3

Interstitial solid solutions

- Fill voids/ interstices

- For high APF, interstitial positions are small. So, atomic diameter of interstitial impurity must be very small (relative to host atoms)

- Max. allowable concentration: <10%

Even very small impurities distort the lattice --->  lattice strains

- Carbon atom: interstitial in Fe

max 2%

Atomic radius of carbon, C: 0.71 Å

Atomic radius of iron, Fe: 1.24 Å

Specification of Composition

A and B atoms

Wt%A=mAmA+mB x 100     m,weightmass

Atom%A=mAAAmAAA+mBAB     mA:mass of A      AA:atomic weight of A

Dislocations- Line defects

- Edge dislocation

- Screw dislocation

Edge dislocation:

Extra half plane of atoms terminates within the crystal

- Dislocation line/extra half plane causes lattice to pull apart.

- Where the extra half plane is not there, the lattice is squeezed together

Screw dislocation:

- Shear stress to distort the lattice

- Upper region is shifted one atomic distance relative to bottom

- Associated spiral or helical ramp

Mixed dislocation: Neither edge perpendicular () or screw  (	    )

Burger’s vector

Close-failure of a dislocation, b (extent of distortion).

Dislocation and b are perpendicular in edge.

They are parallel in screw.

Extra half plane of atoms

b: Burger’s vector

: Edge Dislocation

Edge Dislocation

Screw Dislocation

b points in a closed-packed direction and is equal to atomic spacing(s)

Grain boundaries

- Grain boundaries are regions of impurity concentration

- Light mismatch between grains: small angle grain boundary

Example: tilt boundary

- Grain within a grain: sub-grain; sub-grain boundary

c

Twin Boundary:

Across a grain: mirror-lattice symmetry

- Due to atomic displacement from applied shear forces. e.g., mechanical twins seen in BCC, HCP

- Due to annealing after deformation.

Example: annealing twins seen mostly in FCC

Tilt Boundary

Edge dislocation Series of edge dislocations

- Array of edge dislocations.

- Similar to small angle grain boundary

Both sides are mirror images of each other.

Volume defects

- Pores

- Cracks

- Inclusions

- Other phases

Microscopy

- Microscopy: Macro/Microstructure photomicrographs

- Optical/light microcopy: 2000x

- Transmission electron microscopy: 1,000,000X, very thin foil; fluorescent screen

- Scanning electron microscopy: 50,000X, good depth of field

- Scanning Probe: 3D topography 109 X possible

Grain size

ASTM grain size number

N = 2n-1

n = grain size number

N = Average No. of grain/square inch at 100X

Larger grain size number   Smaller grains

Summary

- Point defects

- Line defects

Edge

- Dislocation	Screw                 				Mixed

- Volume defects

High angle

- Grain boundary   		Low angle

Twin

- Microscopy

- Grain Size