Chapter 5: Diffusion

Introduction

- Material transport by atomic motion

- Diffusion couple:

Example: Cu-Ni in close contact; hold at elevated temperature for extended period and cool to room temperature.

Before

After

- Interdiffusion or impurity diffusion

- Self diffusion: same type of atoms; no composition change

Diffusion mechanisms

Vacancy diffusion

Interstitial diffusion

- Vacancy Diffusion

Atom from normal lattice position changes position with an adjacent vacancy (vacancy lattice site). So, the atoms and vacancies travel in opposite directions. Both self-diffusion and inter (impurity)-diffusion can occur thus

- Interstitial Diffusion

Atoms move from one interstitial site to another (vacant) interstitial site.

Steady state Diffusion

J=MAt

If J is constant, steady-state diffusion exists.

Where,

J	= rate of mass transfer with time, kg/m2-sec or atoms/m2-sec

A	= Area across which diffusion is occurring

t	= elapsed time, sec

Steady-state Diffusion					Concentration Profile

C: Concentration of diffusing species, kg/m3 or gm/cm3

x: Position

Hydrogen gas across palladium plate

Concentration Gradient: Slope at a particular point on the curve

=dCdx

=∆C∆x

=CA-CBXA-XB

Fick’s first law of diffusion

J= -Ddcdx

Where:

D	= Diffusion coefficient, m2/sec

Dc/dx	= Concentration gradient is the main driving force for diffusion

(-)	= Concentration gradient decrease

Example

Carbon diffusing through a plate of iron

5mm

10mm

Carbon

Deficient

Carbon

Rich

Concentration: 1.2 kg/m3   0.8 kg/m3

Diffusion coefficient: 3 x 10-11 m2/sec

J= -DCA-CBXA-XB

= -3x10-11m2sec 1.2-0.85x10-3-10x10-3

=2.4 x 10-9kg/m2sec

Non-steady state Diffusion

- Diffusion flux and concentration gradient vary with time; net accumulation or depletion of diffusing species results

Fick’s Second Law

∂C∂t=∂∂x D∂C∂x

Modified Fick’s Second Law

∂C∂t=D∂2C∂x2

Semi-Infinite solid

Surface concentration at the other end is constant. eg, Bar of length, l > 10Dt , i.e., none of the diffusing atoms reach the bar end during the time-period of diffusion

Assumptions:

- Co = Concentration before diffusion

- x = Distance; at surface it is 0. It increases into the solid

- t = Time; zero(0) at the instant diffusion starts

For t=0 and 0≤x≤	C=Co

For t>0 and x = 0	C=CS (Constant surface concentration)

At x= 		C= CO

∂C∂t=D∂2C∂x2

Cx-C0Cs-C0=1-erfx2Dt

This equation shows relationship between concentration, position and time.

erf = Error Function

CX=Concentration at depth x after time t.

erfx2Dt=erf2

- Concentration at distance x, CX is a function of x2Dt

- If time (t) and position (x) are known and CO, CS and D are given, CX can be determined

If CX=C1 at a specific concentration of solute,

C1-C0Cs-C0=constant

Therefore,

x2Dt=constant

x2Dt=constant

Surface concentration

Concentration C at

distance x

Concentration before

diffusion

Example

Carburization of steel using methane (CH4) at 950°C (1750°F)

Steel:

0.25 wt% Carbon. Using CH4, carbon at surface is suddenly brought to and maintained at 1.2 wt% carbon. How long will it take to achieve a carbon content of 0.80% carbon at a position  0.5 mm below the surface?

D= 1.6 x 10-11 m2/sec

Cx-C0Cs-C0=0.80-0.251.20-0.25=1-erf5x10-4m21.6x10-11 m2/sec

0.4210=erf62.5st

| z | erf (z) |
| --- | --- |
| 0.35 | 0.3794 |
| z | 0.4210 |
| 0.40 | 0.4284 |

z-0.350.40-0.35=0.4210-0.37940.4284-0.3794

Or

z=0.392

Therefore,

62.5st =0.392

And solving for t,

t=62.5s0.3922=25400 seconds=7.1 hours

Example

The diffusion coefficients for copper in aluminum at 500 and 600 C are 4.8x10-14 and 5.3x10-13 m2/s, respectively. Determine the approximate time at 500 C that will produce the same diffusion result (in terms of concentration of Cu at some specific point in Al) as a 10-h heat treatment at 600°C.

To produce the same effect at 500°C, how long will it take?

Dt = constant

D500t500=D600t600

t500=D600t600D500=5.3x10-13m2s10 h4.8x10-14m2s=110.4 hours

Factors in diffusion

- Temperature

- Time

D increases 5 orders of magnitude with temperature.

D=Doexp-QdRT

Where:

Do   	= temperature independent pre-exponential (m2/sec)

Qd 	=  the activation energy for diffusion (J/mol,cal/mol and ev/atom)

R   	= gas constant, 8.31 J/mol-K or 8.62 eV/atom-K

T   	= absolute temperature (K)

lnD=lnDo-QdR 1T

Where:

From the equation y=mx+b,

y	= ln D

mx	= 1/T

b 	= ln Do

Summary

- Self Diffusion

- Inter-Diffusion

- Steady state 	J=M/At    Fick’s First law

- Non-steady state  Fick’s second law

- Temperature effect

- Activation energy