Chapter 13: Ceramics and Properties of Ceramics

Root: keramikos (Greek for “burnt stuff”)

Traditional Ceramics: china, porcelain, bricks, tiles, glasses and high temperature ceramics

New generation ceramics: (Since better understanding of the fundamental character of ceramics, and parameters influencing their unique properties)

Impact: electronic, computer, communication, aerospace and other industries.

CERAMIC STRUCTURES: composed of electrically charged ions; not atoms. Partial or total ionic bonding.

Cations: metallic ions, positively charged, since they have given up valence electrons to non-metallic ions.

Anions: non-metallic ions, negatively charged

CRYSTAL STRUCTURES: Influenced by two characteristics:

- Magnitude of the electrical charge on each of the component ions. The crystal must be electrically neutral. ie., balancing of positive and negative charges.

- Relative sizes of Cations and Anions. Ionic radii: rccation and raanion

Since they give up electrons, Cations are usually smaller than Anions. : rc/ra <1

Each ion desires to have as many nearest neighbours of the opposite charge. Stable when anions are touching a cation.

Coordination No: number of anion nearest neighbours of a cation.                                                   P. 378-379 Table 13.1:

Example:

Show that the minimum cation to anion radius ratio for the coordination number 3 is 0.155.

AP=rA

AO= rA + rC

cos (30o)=AP/AO= rArA+rC =√32

rCrA=1-√3/2√3/2=0.155

Types of Structures

AX-Type Crystal Structure

- Equal number of cations and anions

- Several different crystal structures for AX compounds

- AX-Rock Salt Structure: NaCl/Rock salt

- Coordination number for anions and cations: 6

- cation/anion ratio: 0.414-0.732

FCC arrangement of anions

Two interpenetrating FCC lattices

FCC arrangement of cations

Examples: NaCl, MgO, MnS, LiF and FeO

- AX - Cesium Chloride Structure: CsCl

- Coordination number for both ions: 8

- Anions at centres of cube

- Cation at body (cube-centre)

- AX – Zinc Blende Structure: ZnS/sphalerite/Zinc Blende

- Coordination number: 4

- S atoms: at cube corners and face positions

- Zn atoms: interior tetrahedral positions, Each Zn atom is bonded to four S atoms and vice versa. Often highly covalent. eg. ZnS, ZnTe, SiC

- Type Crystal Structures

- m and/or p ≠ 1

- eg. AX2: CaF2/Flourite

- Coordination Number: 8 	rc/ra = 0.8

- Similar to CsCl structure. But, only half as many Ca2+ as F+ ions so, only half the centres cube positions are occupied by Ca2+ ions.

- Examples: UO2, PuO2 and ThO2

- AmBnXp Type Crystal Structure ("Two types of cations”)

Examples: BaTiO3/Barium Titanate

Ceramic Density Calculations

From page 36,

=nAVCNA

Where:

n	= number of atoms associated with each unit cell

A	= atomic weight

Vc 	= Volume of the unit cell

Na 	= Avagadro’s number (6.023 x 10^23 atoms /mole)

=n'Ac+AAVCNA

Where:

n' 	= the number of formula units within the unit cell (eg.BaTiO3: 1, 2 ,3)

AC	= the sum of the atomic weights of all cations in the formula unit

AA 	= the sum of the atomic weights of all the anions in the formula unit

VC 	= the unit cell volume

NA	= Avagadro’s number

Example:

Compute the theoretical density of NaCl on the basis of crystal structure.

How does this compare with its measured density?

n' 	= 4/unit cell

AC 	= ANa

= 22.99 g/mol

AA 	= Acl

= 35.45 g/mol

Vc 	= a3

a 	= 2(rNa + rcl)

rNa	= 0.102 nm

rcl 	= 0.181nm

=n'(ANa+ACl)(2rNA++2rCl-)3NA

=4(22.99+35.45)(2(0.102×10-7)+2(0.181×10-7)3NA

=2.14 g/cm3

Expected value: 2.16 g/cm3

Ceramic Phase Diagrams

The Al2O3-Cr2O3 System

Isomorphous (density similar to Cu-Ni)

- Fig. 13.24: Al2O3-Cr2O3 Substitution Solid Solution. (Al3+ substitutes for Cr3+), same charge.

- Similar radii: 0.053nm  (Al3+)	0.063 nm (Cr3+)

- Same crystal structure

The MgO-Al2O3 System (similar to Pb-Mg)

- Intermediate phase: MgAl2O4 spinel (ie., MgO-Al2O3)

- Fig.13.25: Distinct compound, single phase field (not a line as for Mg2Pb)

- Spinel nonstoichiometric (range of compositions)

- Differences in charge: 	Mg2+				Al3+

0.072 nm (Mg2+)	             0.053 nm (Al3+)

- MgO is virtually insoluble in Al2O3; so no terminal solid solution at RHS

- Two eutectics

- Constant melting of spinel at 2100°C

The ZrO2-CaO System (zirconia/calcium)

- Three reactions: eutectic, pertectic and eutectoid.

- Three different crystal structures: tetragonal, monoclinic, cubic

- Pure ZrO2: tetragonal to monoclinic at 1000°C

a= b ≠ c	    	      a ≠ b ≠ c

α = β = γ = 90° 	 α =  γ = 90° ≠ β

Results in cracking so, “stabilize” by adding 3 to 7 wt.% CaO to ZrO2. This eliminates cracking,

as no such phase change occurs.

The SiO2-Al2O3 System

- SiO2 and AL2O3: Not mutually soluble

- No terminal solid solutions at both extremities

- Si02: cristobalite (most stable form)

- 3Al2O3-2SiO2: Mullite

- Simple eutectic at 1587 oC

Plastic Deformation

Crystalline Ceramics:

- Why are crystalline ceramics hard and brittle?

- Few slip systems for the movement of dislocations (due to the electrically charged nature of ions).

- Electrostatic repulsion of like charges eliminates several possibilities of slip (disloc. motion)

- Deformation by motion of dislocations

- Hard and brittle :difficulty in dislocation motion (slip)

- Bonding: ionic; therefore few slip systems (planes and directions) for dislocation motion, due to electrically charged nature of ion.

- For slip in some direction, ions are brought close to one and other; but this type of motion is restricted due to electrostatic repulsion

- For ceramics with covalent bonding, slip is difficult because:

- Covalent bonds are strong

- Limited no. of slip systems

- Dislocation structures are complex

Noncrystalline Ceramics (glassy)

- Deformation is not by dislocation motion

- But by viscous flow

- Rate of deformation  applied stress

- Atoms/ions slide past one another by breaking/reforming bonds

- Viscosity: measure of resistance to deformation

τ=F/A

η=τdv/dy=F/Adv/dy

Where:

η, viscosity. Poises (P) pascal-second

τ, Applied shear stress

dv, change in viscosity

dy, distance in direction perpendicular to and away from plates.

1Poise

1 P	=1 dyne-second/cm2

1Pa-s	=1N-sec/m2

10 P	=1 Pa-s

Water: 10-3 Pa-s

Glass: very large (since strong interatomic bonding). As temperature increases, the magnitude of bonding is diminished, sliding motion or flow of atoms or ions is facilitated, then there is a decrease in viscosity.