Chapter 14: Polymer Structures

Hydrocarbon Molecules

Unsaturated: Double and triple bonds

|  | CnH2n | CnH2n-2 |
| --- | --- | --- |
| Examples: | Ethylene | Acethylene |
|  | CH2=CH2 | CHCH |
|  | C2H4 | C2H2 |

Saturated: single bonds

Examples: 	CH4,C2H6, C3H8

CnH2n+2

Isomerism: 	n-butane 		Isobutane

Straight chain		Branched chain

Polymer Molecules

Gigantic: 	Macromolecules

Monomer: 	One unit

Polymer: 	Many units

Example: one unit

PTFE: 	TEFLON (Polytetrafluoro ethylene)

PVC: 	Vinyl (Polyvinyl chloride)

Polypropylene:

Homopolymer:	Repeating units of the chain are of the same type.

Co-polymer: Two or more different mer units.

Bifunctional: Two (2) active bonds

Trifunctional: Three (3) active bonds

Molecular weight

- Large macromolecules synthesized from molecules

- Not all polymer chains grow to the same length

- Average molecular weight is determined by measuring viscosity and osmotic pressure

- The chain is divided into size ranges

- No. of moles (or fraction) of each size range is determined

Number average molecular weight,       =xiMi

Where:

Mi	= Mean molecular weight within a size range

xi	= Fraction of number of chains within the corresponding (same) size range

Weight Average Molecular weight,	 =wiMi

Where:

Mi	= Mean molecular weight within a size range

wi	= weight fraction of molecules within the same size range

Notice the shift!

Degree of polymerization (n):

n	= Average no of mer units in a chain

nn	= Number average degree of polymerization

nw	= Weight average degree of polymerization

nn=Mnm                             m=Mer molecular weight

nw=Mwm

For a copolymer (i.e., two or more mer units),

m= Σ fj mj

Where:

fj	= chain fraction of mer

mj	=molecular weight of mer

Example:

Computations of Average Molecular Weights and Degree of Polymerization

Assume that the molecular weight distributions shown in Figure 14.3 are for poly(vinyl chloride). For this material, compute:

(a) the number-average molecular weight,

(b) the degree of polymerization, and

(c) the weight-average molecular weight.

xiMi=21,150

Where, xi: Fraction of total no. of chain within the corresponding size change

: Number average molecular weight

xiMi=23,200

Where, 	          : weight average molecular weight

PVC: C2H3Cl

|  | C | H | Cl |
| --- | --- | --- | --- |
| Atomic Weight (g/mol) | 12.01 | 1.01 | 35.45 |

m=212.01+31.01+35.45

m=62.50 g/mol

Number average degree of polymerization,

nn=Mnm=2115062.50=338

Molecular weight of polymers

- Melting point increases with molecular weight (forup to 100,000 g/mol).

Ie. increased intermolecular forces

- Long chain  increased bonding between molecules. (Van der Waals or hydrogen bond)

- At room temperature,

Short chains: Molecular weight: 100 g/mol – liquids/gases

(1000 g/mol: waxes, soft resins)

High polymers: 10,000 to several million g/mol – solids

Molecular shape

- Single chain bonds can rotate like a cone/bend in three dimensions

- Bends, twists, kinks, in single chain molecules

C  C: rigid (rotationally)

Bulky or large side group: restricted rotation

Benzene ring: restricted rotation

Molecular structure

Linear Mer units end-to-end in chains

Examples:

Polyethylene	PVC

Polystyrene

PMMA

Poly(methyl methacrylate)

Branched Polymers

- Side-branch chains

- Less packing efficiency; lower density

Cross-linked Polymers

- Formed by non-reversible chemical reaction

- Additives covalently bonded to chains

Example: sulfur in vulcanizing

Net-work polymer

- Three active covalent bonds

- Highly cross-linked

Molecular configurations

Head-to-tail configuration

: Bonded to alternate carbons on the same side

Where, R: Alkyl radical

Head-to-head configuration

: Bonded to adjacent carbon atoms

Stereoisomerism

Isotactic configuration

: R groups are situated on the same side of the chain

Syndiotactic

: On alternate sides

Atactic

: At random position

Conversion from to another is only by severing branches and through new reaction..

Geometric Isomerism

CIS-Isoprene

ExampleL Natural rubber

Attacked by acids/alkalis

TRANS-Isoprene

ExampleL Gutta Percha

Highly resistant to acid/alkalis

TRANS- isoprene

Example:  Gutta Percha

Highly resistant to acids/alkalis

Copolymers (different types of mers)

Random

Alternate

Block

Styrene butadiene rubber (SBR), (Random copolymer): Automobile tires.

Nitrile butadiene rubber (NBR), Random copolymer): Gasoline hose

Polymer Crystallinity

Crystallinity: Packing of chains to produce ordered atomic array.

% Crystallinity=ρcρs-ρaρsρc-ρa x 100

Where:

ρs = Density of specimen

ρa = Density of totally amorphous polymer

ρc = Density of perfectly crystalline polymer

Crystallinity characteristics

- Degree of crystallinity depends on rate of cooling; need sufficient time to result in ordered configuration.

- Amorphous (No crystallinity) if chemically complex microstructure. Crystalline if chemically simple polymer.

Example: polyethylene, PTFE, even if rapidly cooled

- Amorphous if network polymer. Crystalline if linear polymer (no restrictions to prevent chain alignment)

- Amorphous: Atactic stereoisomer. Crystalline: Isotactic or Syndiotactic stereoisomer

- Amorphous: If bulky/large side-bonded group. Crystalline: Simple straight chain

- Amorphous: Most copolymers (and more irregular/ random mers)

- Crystalline: Alternating or block polymers

- Amorphous: Random or graft polymers

- Crystalline: Strong, more resistant to dissolution by softening by heat

Polymer crystals

Fringed micelle model

- Aligned small crystalline regions (crystallites or micelles)

- Amorphous regions in-between platelets of crystals (10-20 nm thick) (10m long)

So, multilayered structure

Chain-fold model: amorphous molecular chains within platelets; back and forth

Spherulite model

- Bulk polymers solidify as small spheres (Spherulites)

- Within each such sphere, folded crystallites (lamellae), ~10 nm thick form

- Adjacent spherulites impinge on each other forming planar boundaries                                                           Example: Polyethylene, Polypropylene, PVC, PTFE, Nylon

Summary of Polymers

- Large molecules of polymers

- Mers, homopolymers, copolymers

- Molecular weight

Number-Average

Weight-Average

- Isomerism

Isotactic

Syndiotactic

Atactic

- Crystallinity: Degree of crystallinity

- Polymer crystals

Thermosetting and Thermoplastic Polymers

Determined by mechanical behavior upon heating to high temperatures

| Thermosetting | Thermoplastic |
| --- | --- |
| Thermosets Become permanently hard upon heating. Do not soften upon subsequent heating. | Thermoplasts Soften upon heating; harden upon cooling. It is reversible. Fabricated by applying heat and pressure. |
| Initial Heating: Covalent crosslink form and link adjacent molecular chains. Chains are anchored; no vibrational or rotational chain motions, 10 – 50% of chain mer units are cross-linked. | As Temperature is Increased: Secondary bonds break (due to molecular motion). So when stress is applied, adjacent chains move. |
| Further Heating: Severance (breaking) of crosslink bonds and polymer degradation. | Irreversible Degradation Upon Further Heating: Violent molecular vibrations break primary covalent bonds. |
| Thermoset polymers are harder, stronger and brittle. Better dimensional stability. Example: Cross linked and network polymers (Vulcanized rubbers, epoxies and phenolic and some polyester resins) | Soft and Ductile. Most linear polymers and polymers with branched structures with flexible chains. |