Lab 5 – CIVE 2200

| 1 . Table 1 Raw Data |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Specimen | Base (mm) | Height (mm) | Area (mm2) | Moment of Inertia (mm4) | r (mm) |
| 1 | 12.75 | 6.12 | 78.03 | 243.5472 | 1.766692 |
| 2 | 12.75 | 6.12 | 78.03 | 243.5472 | 1.766692 |
| 3 | 12.8 | 6.4 | 81.92 | 279.6203 | 1.847521 |
| 4 | 12.4 | 6.45 | 79.98 | 277.2807 | 1.861955 |
| 5 | 12.12 | 6.25 | 75.75 | 246.582 | 1.80422 |
| 6 | 12.7 | 6.5 | 82.55 | 290.6448 | 1.876388 |
| 7 | 12.5 | 6.35 | 79.375 | 266.7165 | 1.833087 |
| 8 | 12.35 | 6.3 | 77.805 | 257.34 | 1.818653 |
| 9 | 12.72 | 6.18 | 78.6096 | 250.1908 | 1.784012 |
| 10 | 12.78 | 6.2 | 79.236 | 253.8193 | 1.789786 |

|  |  | Theoretical |  | Experimental |  |
| --- | --- | --- | --- | --- | --- |
| L' (mm) | L'/r | P' (kN) | σ'(MPa) | P (kN) | σ(MPa) |
| 118.8 | 67.24433 | 34.06111585 | 436.5130828 | 17.44 | 223.5038 |
| 144.6 | 81.84789 | 22.99085735 | 294.6412579 | 18.76 | 240.4204 |
| 168 | 90.93267 | 19.55503644 | 238.708941 | 14.91 | 182.0068 |
| 193 | 103.6545 | 14.69310265 | 183.7097105 | 12.49 | 156.164 |
| 249 | 138.0098 | 7.850029326 | 103.6307502 | 8.56 | 113.0033 |
| 290.5 | 154.8187 | 6.797963352 | 82.3496469 | 5.85 | 70.86614 |
| 351 | 191.4803 | 4.273111818 | 53.83447959 | 3.85 | 48.50394 |
| 216 | 118.7692 | 10.88700457 | 139.9267987 | 10.02 | 128.7835 |
| 197 | 110.4252 | 18.17813589 | 231.2457498 | 25.66 | 326.4232 |
| 173 | 96.65961 | 33.47888713 | 422.5211663 | 27.46 | 346.5596 |

Sample Calculations (Include calculations for Specimen 1)

I = bh312 = 12.75*(6.12)312 = 243.5472 mm4	r =I/A = 243.5472/78.03 = 1.766692 mm

P’cr =π2EI(KL)2			 σ'cr=π2E(L'r)2 		σcr= PcrA

= 	π2200*103(243.5472)(1*118.8)2	          = π2(200*109)67.2442	       = 17.44*10378.03

= 34.061 (kN)	           	          = 436.513 (MPa)      = 223.5038 (MPa)

Discussion

2.  For Specimens 2-8, 10 the theoretical and experimental critical loads are within approximately 4 kN of one another. However, the theoretical critical load for Specimen 1 is 34.06 kN but, the experimental load is only 17.44 kN. The theoretical load of 34.06 kN corresponds to what kind of load we would expect to see since specimen 2 which had a length of 144.6 mm had a critical failure of 18.76 kN. A possible reason for the low load at failure is that the beam had been previously subjected to some sort of axial compression previous to testing. If the beam had buckled during any previous load application like in transportation or manufacturing, the critical load would decrease. The critical load would decrease because, by previously applying a load, the beam will lose strength in its elastic region, reaching the strain necessary for failure much quicker. Specimens 2-8 experienced similar experimental and theoretical critical failure loads. However, all theoretical loads other than specimen 4 (and specimen 9) were higher than the experimental loads. One reason for this difference could be previous internal strains experienced during transportation or handling. This would make the specimen weaker since some strength would already have been lost when a load was applied.

3. L’/r vs. Stress graph below. (Graph 1)

4. Table 2. Comparison of experimental length factor K to theoretical values.

| L (mm) | I (mm^4) | Pcr (N) | K |  |
| --- | --- | --- | --- | --- |
|  |  |  | experimental | theoretical |
| 216 | 257.34 | 10020 | 1.04 | 1 |
| 197 | 250.1908 | 25660 | 0.704 | 0.7 |
| 173 | 253.8193 | 27460 | 0.781 | 0.5 |

Sample calculation of Kexp using specimen 8

K  =π2⋅E⋅IPcrL   K = π2⋅(200,000)(106)⋅(257.34)1002021600   K =1.042391609     K= 1.04

The experimental length factor K is very close to the theoretical K value for specimens 8 and 9 however, the experimental K value for specimen 10 was much higher than the theoretical value of 0.5. This may be due to the fact the buckling load (Pcr) for specimen ten significantly lower than expected, also as seen in graph 1, the experimental stress was significantly lower than the theoretical stress.